Ultrasonic Synthesis of Polymeric Ionic Gels for Semi-Solid-State Batteries

Research institution: Universidad de Valladolid Science Park | UVa Foundation

Principal investigator: Prof. Dr. Pablo Martín-Ramos

Co-principal investigator: Prof. Dr. Jesús Martín-Gil

# EXECUTIVE SUMMARY

Electrochemical energy storage is critical for Spain’s decarbonization roadmap, with PNIEC 2021–2030 targeting 6 GWh of storage capacity by 2030 to support 60–80% renewable penetration. Semi-solid-state batteries (semi-SSB) offer a strategic technology pathway bridging conventional Li-ion systems and next-generation all-solid-state devices, delivering higher energy density, improved thermal safety, and lower projected manufacturing costs compared to both incumbent technologies and emerging solid-state alternatives.

The problem: Current gel electrolyte manufacturing relies on passive deposition methods (doctor-blade, spin-coating, drop-casting) that trap micro-voids during solvent evaporation, creating interfacial impedance barriers exceeding 500–1000 Ω·cm2 that severely limit ion transport kinetics and reduce practical cycle life. This manufacturing bottleneck prevents gel-based systems from achieving their theoretical performance potential and blocks commercialization pathways.

Our solution: This proof-of-concept validates a dual-stage ultrasonic manufacturing process: (i) acoustic cavitation synthesis of high-conductivity polymeric ionic gels with controlled nanoparticle dispersion, and (ii) direct sonotrode consolidation onto electrode layers to eliminate microporosity and ensure continuous ionic contact. This combined methodology represents a fundamental departure from passive deposition approaches and is protected by Spanish patent application P202630136.

Technology readiness: The project advances from TRL 3 (experimental proof of concept with isolated component validation) to TRL 5 (laboratory-scale validated prototype with integrated cell performance), with clear pathways to industrial scale-up through established partnerships with Graphenea (graphene supply), Basquevolt (cell manufacturing), and Phi4Tech (electrolyte formulation licensing).

Key deliverables: (i) Reproducible gel formulations (ionic conductivity ≥0.5 mS·cm−1, mechanical strength ≥10 MPa, batch homogeneity ≥95%); (ii) validated sonotrode consolidation protocol achieving interfacial impedance <100 Ω·cm2; (iii) full-cell electrochemical validation: 100 cycles at C/5 rate with ≥80% capacity retention (with extended cycling pathway to 200 cycles documented); (iv) ISO 14040/44 life-cycle assessment targeting 8–12% CO2-eq reduction vs. thermal synthesis; (v) industrial viability analysis (COGS <€300/kWh at pilot scale) with identified commercialization partners.

# EVOLUTION OF PRIOR RESEARCH

## Foundation: team research trajectory

This proof-of-concept builds directly upon a decade of systematic research in ultrasonic-assisted materials synthesis conducted by the PI and Co-PI at Universidad de Valladolid. The research foundation includes:

Ultrasonic synthesis methodology: the team has published approximately 30 peer-reviewed articles on sonication-assisted synthesis of nanostructured materials, polymeric systems, and functional coatings. Key publications demonstrate: acoustic cavitation parameters for controlled nanoparticle dispersion; temperature management during high-energy sonication; and polymer-nanoparticle interface optimization.

Electrochemical materials development: recent work (2022–2025) has specifically targeted energy storage applications: graphitic carbon nitride (g-C3N4) synthesis and characterization for electrochemical systems; carbon-nitrogen composite materials for electrode enhancement; solid-state ionic conductors and polymer electrolytes.

Technology maturation: The team’s expertise has progressed from fundamental acoustic physics to applied materials synthesis to device-level integration—exactly the trajectory required for a proof-of-concept project targeting industrial transfer.

## Intellectual property foundation

The core innovation is protected by Spanish patent application P202630136, with Prof. Martín-Ramos and Prof. Martín-Gil as inventors. The patent covers: dual-stage ultrasonic processing methodology for gel electrolyte synthesis and electrode consolidation; specific parameter windows for acoustic cavitation optimization; and an integration protocol for multi-component cell assembly. This intellectual property protection demonstrates that the technical approach is validated, documented, and recognized as innovative. The patent provides the foundation for licensing discussions already initiated with Basquevolt and Phi4Tech.

## Gap analysis: from laboratory results to industrial relevance

Prior research has validated individual components (gel conductivity, nanoparticle dispersion, consolidation physics) but has not integrated these elements into complete electrochemical cells with systematic cycling validation. The specific gap this PoC addresses:

| Validated (prior research) | To be validated (this PoC) |
| --- | --- |
| Single-component gel synthesis | Three-component integrated system |
| Isolated conductivity measurements | Full-cell impedance and cycling |
| Laboratory-scale batches (~5g) | Reproducibility validation (100g scale) |
| Academic characterization | Industrial-grade LCA and COGS |

This PoC provides the essential bridge from academic proof to industrial transfer readiness.

# PROOF-OF-CONCEPT QUALITY AND VIABILITY

## Strategic context and manufacturing gap

Spain and the EU must dramatically increase electrochemical storage capacity to accommodate 60–80% renewable energy penetration by 2030. The EU Battery Regulation (2023/1670) mandates carbon footprint labeling, creating regulatory pressure for sustainable manufacturing processes. Semi-SSB represent an accessible commercial pathway: they achieve 230–260 Wh/kg energy density (vs. 180–220 Wh/kg for conventional Li-ion) while avoiding the extreme manufacturing challenges of all-solid-state systems (specialized dry rooms, high-pressure sintering at 700°C+, novel sulfide/oxide electrolyte handling).

Manufacturing gap: current literature optimizes gel electrolytes in isolation using conventional deposition methods—doctor-blade coating, spin-coating, and drop-casting. These approaches share a fundamental limitation: solvent evaporation from a static film inevitably traps micro-voids at the electrode-electrolyte interface. These voids create ionic transport barriers, with interfacial impedance often exceeding 500–1000 Ω·cm2, which limits practical charge/discharge rates and accelerates capacity fade.

While ultrasonic synthesis of nanoparticle dispersions is well-established, no systematic methodology exists for ultrasonic consolidation (direct sonotrode application to wet-coated electrode layers) applied across all three gel components (bulk electrolyte, anode coating, cathode coating) with integrated full-cell electrochemical validation. This gap represents our innovation opportunity and defines the PoC scope.

## Three-component gel system: technical architecture

The project develops a modular, ultrasonically synthesized system with engineered electrochemical functionality across three components:

1. Bulk electrolyte gel:

- Polymer matrix: polyvinylidene fluoride hexafluoropropylene copolymer (PVDF-HFP), providing mechanical strength, electrochemical stability (up to 4.5V), and ionic transport pathways.

- Ionic carriers: lithium salts (LiPF6 for proven performance; LiFSI for enhanced high-voltage stability) dissolved at 0.8–1.2 M concentration.

- Plasticizer system: ethylene carbonate/dimethyl carbonate (EC:DMC, 1:1 v/v) for Li+ solvation.

- Nanofillers: silicon dioxide nanoparticles (SiO2, 5–10 wt%) providing dual functionality: mechanical reinforcement (target strength ≥10 MPa) and dendrite suppression through interfacial interactions.

- Target performance: ionic conductivity σ ≥0.5 mS·cm−1 at 25°C.

2. Anode-protective coating:

- Electronic conductor: commercial Graphenea graphene sheets (10-layer, 99.5% purity).

- Critical innovation: g-C3N4 nanosheets at 2–5 wt% loading, providing N-doped active sites that accelerate lithium-ion desolvation kinetics at the anode-electrolyte interface through Lewis acid-base interactions and suppress dendritic electrodeposition through favorable Li+ coordination.

- Binder: PVDF or polyacrylic acid derivative (5–8 wt%) for mechanical adhesion.

- Target performance: Interfacial impedance <100 Ω·cm2 (vs. >500 Ω·cm2 for conventional coatings).

3. Cathode-protective coating:

- Active material: conventional lithium cobalt oxide (LiCoO2) or lithium nickel-manganese-cobalt oxide (NMC) particles.

- Protective shell: mixed-oxide composition (Al2O3/SiO2, 50–200 nm thickness) suppressing oxygen release from layered oxide structure and stabilizing the cathode-electrolyte interphase (CEI).

- Binder: PAA/PVDF blend for structural integrity.

- Target performance: capacity fade ≤0.15% per cycle.

## Critical innovation: ultrasonic consolidation mechanism

The key differentiator of this PoC is non-contact acoustic infiltration via a coupling bath (Patent P202630136). Unlike direct probe sonication—which risks damaging delicate electrode structures—our method submerges the wet-coated stack in an inert coupling fluid. The ultrasonic probe transmits energy through this fluid without physical contact with the stack.

Physical mechanism: directed acoustic pressure waves propagate through the coupling liquid and drive the viscoelastic gel into the electrode's microporosity via a controlled 'pumping effect', achieving complete interfacial densification while preserving layer integrity—a capability impossible with static pressing or direct-contact methods. The coupling liquid is maintained below 35°C via circulation/refrigeration to prevent thermal degradation.

Result: continuous void-free ionic contact pathways with dramatically reduced interfacial impedance—the fundamental bottleneck limiting current gel electrolyte performance.

## Methodology and experimental design

Design-of-experiments approach (SO1). Comprehensive factorial DoE varying:

- Ultrasonic frequency: Fixed 20–24 kHz (probe sonication)

- Acoustic amplitude: 30–90% (consolidation restricted to 30–60% to minimize thermal/mechanical degradation)

- Sonication duration: 5–30 minutes effective exposure, pulse mode as needed

- Processing temperature: 20°C, 30°C, 40°C

- Measured responses: Ionic conductivity (EIS, 10 mHz – 1 MHz); mechanical properties (tensile testing ASTM D882, shore-D hardness); morphological assessment (SEM cross-sections at 5000×); interfacial adhesion (ASTM C1624 scratch testing).

Full-cell validation (SO2–SO3). CR2032 coin-cells across selected architectures:

- Li-ion chemistry: LiPF6-based (reference); LiFSI-based (high-voltage)

- Na-ion chemistry: NaPF6-based (sustainability pathway)

- Electrode variants: conventional graphite/LiCoO2 vs. graphene+g-C3N4/CEI-stabilized cathode

- Replication: n=3–5 per configuration for statistical validity

Electrochemical protocol:

- Formation cycling: 50 cycles at C/20 rate (25°C)

- Extended cycling: 100 cycles at C/5 rate with EIS every 25 cycles

- Thermal stress: parallel cycling at 50°C (accelerated aging)

- Post-mortem: glove-box disassembly, SEM-TEM imaging of interfaces

## Risk mitigation strategy

| Risk | Prob. | Impact | Mitigation | Contingency |
| --- | --- | --- | --- | --- |
| Ionic conductivity below target (<0.5 mS·cm−1) | Medium | High | Expand DoE parameter space; alternative salt formulations (LiFSI, LiTFSI); optimize SiO2 loading | Accept 0.3 mS·cm−1 minimum with documented improvement pathway |
| Thermal degradation during sonication | Medium | Medium | In-situ thermal monitoring (IR camera); pulse-mode operation; amplitude reduction | Shift to bath-type sonication with lower intensity; pre-cooling protocols |
| Risk | Prob. | Impact | Mitigation | Contingency |
| g-C3N4 dispersion inhomogeneity | Low | Medium | Pre-dispersion ultrasonication; surface functionalization | Alternative N-doped carbon materials |
| Scale-up reproducibility challenges | Medium | High | 100g validation batches with statistical process control (≥95% homogeneity, ≤5% inter-batch variability) | Partner with CIC EnergiGUNE for scale-up troubleshooting |
| Partner disengagement | Low | Medium | Maintain parallel discussions with multiple industrial contacts | Pivot to alternative licensing/spin-off pathway |

# TIMELINE AND MILESTONES

## Phase structure (24 months)

The project is structured in four overlapping phases designed to maximize parallel efficiency while maintaining logical dependencies:

Phase 1 (M1–M8): synthesis optimization and consolidation parameter definition

- M1–M2: DoE design finalization; equipment calibration; material procurement.

- M2–M4: synthesis of 45–60 gel formulations per DoE plan.

- M3–M5: sonotrode consolidation mapping with in-situ thermal monitoring.

- M4–M6: comprehensive characterization (TGA-DSC, SEM-EDS, FTIR).

- M5–M6: statistical regression analysis; optimal formulation identification.

- Milestone M6: synthesis optimization complete—σ ≥0.5 mS·cm−1, strength ≥10 MPa, SOP validated.

Phase 2 (M7–M16): electrode integration and cell validation

- M7–M8: electrode coating with optimized formulations; consolidation verification.

- M8–M10: coin-cell assembly (selected architectures); formation cycling.

- M10–M12: extended galvanostatic cycling (25°C); EIS tracking.

- M12–M14: thermal cycling (50°C); safety testing (ARC, nail penetration).

- M14–M16: cell disassembly; post-mortem SEM-TEM analysis.

- Milestone M16: cell validation complete—≥80% retention at 100 cycles; safety data; manuscript draft.

Phase 3 (M13–M20, parallel with Phase 2): LCA and industrial transfer

- M13–M16: LCA data collection and OpenLCA modeling.

- M16–M18: COGS model construction at multiple scales.

- M18–M20: industrial partner engagement (Basquevolt, Phi4Tech, Iberdrola).

- Milestone M18: LCA finalized; COGS study complete; letters of intent obtained

Phase 4 (M19–M24): reproducibility validation and dissemination

- M19–M20: 100g validation batch synthesis with statistical process control.

- M20–M22: PCT patent filing; manuscript preparation.

- M23–M24: final reporting; conference presentations; partnership agreements.

- Milestone M24: Project completion—publication submitted; PCT filed; SOPs finalized.

## Deliverable alignment with prize requirements

| Deliverable | Timeline | Reporting |
| --- | --- | --- |
| Intermediate scientific-technical report | M12 | Phase 1 complete; Phase 2 in progress |
| Final scientific-technical report | M25 (within 30 days of completion) | Complete dataset; LCA; COGS; commercialization roadmap |
| Economic justification report | M25 | Detailed expense documentation |

Detailed Gantt chart and monthly activity breakdown are provided in the separate Calendar document.

# BUDGET ADEQUACY

## Budget summary

| Category | Amount (€) | Percentage |
| --- | --- | --- |
| Personnel | 65,000 | 65% |
| Characterization services | 25,000 | 25% |
| Materials and consumables | 10,000 | 10% |
| TOTAL | 100,000 | 100% |

## Personnel justification (€65,000)

Junior Researcher (MECES Level 4 / Doctor <4 years experience):

- Monthly base salary: €2,056.39

- Social contributions (31.65%): €650.85

- Monthly employer cost: ~€2,707

- 24-month total: €64,968 ≈ €65,000

This dedicated researcher provides essential continuity across all four project phases: synthesis execution, electrochemical testing, characterization coordination, data analysis, and reporting. The junior researcher profile ensures appropriate scientific training while maintaining cost efficiency.

Note: Senior researchers (PI, Co-PI, extended team) contribute through existing Universidad de Valladolid positions at no direct cost to the prize budget, leveraging institutional co-funding to maximize research output per euro invested.

## Characterization services (€25,000)

| Service | Cost (€) | Justification |
| --- | --- | --- |
| SEM-EDS | 9,000 | Cross-sectional morphology; void verification; ~50 samples |
| TEM | 5,000 | High-resolution interfacial imaging; SEI/CEI characterization |
| TGA-DSC | 3,500 | Thermal stability profiling; ~30 samples |
| ARC | 3,000 | Thermal runaway onset; safety validation |
| LCA + COGS modeling | 2,500 | OpenLCA, ecoinvent access, ISO compliance consultation |
| Patent support (PCT) | 2,000 | International filing preparation; claims review |

## Materials and consumables (€10,000)

| Item | Cost (€) |
| --- | --- |
| Chemical precursors (PVDF-HFP, Li salts, solvents) | 3,500 |
| Commercial graphene (Graphenea) | 2,500 |
| g-C3N4 nanofillers | 2,000 |
| Coin-cell hardware and assembly materials | 2,000 |

## Cost optimization strategy

- No indirect costs: 100% of the prize budget flows directly to research activities.

- Institutional leverage: UVa provides facility overhead, administrative support, and senior researcher time.

- Partnership rates: IMDEA provides advanced characterization at reduced academic rates.

- DoE efficiency: Statistical optimization minimizes wasted experiments.

Detailed budget breakdown with phase-by-phase allocation is provided in the separate budget document.

# TEAM CAPACITY

## Principal investigator

Prof. Dr. Pablo Martín-Ramos: Full Professor, Universidad de Valladolid; Director of Consolidated Research Unit UIC-262.

Qualifications: 203 JCR-indexed publications (h-index: 33); research focus on materials synthesis, polymer science, electrochemical systems; multiple patents in materials engineering and electronic technologies; co-inventor of patent P202630136 (core project IP); extensive experience in industrial R&D collaboration

Project role: overall scientific direction; synthesis methodology development; electrochemical validation oversight; industrial partnership coordination. Dedication: 30% FTE.

## Co-principal investigator

Prof. Dr. Jesús Martín-Gil: Emeritus Professor, Universidad de Valladolid.

Qualifications: over 300 peer-reviewed publications; extensive industrial R&D experience in chemical manufacturing and process engineering; co-inventor of patent P202630136; track record in technology transfer and scale-up.

Project role: large-scale synthesis optimization; process engineering expertise; technology transfer guidance. Dedication: 15% FTE.

## Extended research team

| Member | Affiliation | Expertise | Project role | Dedication |
| --- | --- | --- | --- | --- |
| P. Chamorro-Posada | UVa | Spectroscopy, data analysis | FTIR characterization; impedance interpretation | 15% FTE |
| R.C. Dante | External collaborator | g-C3N4 synthesis | Anode formulations | 10% FTE |
| M. Avellá | IMDEA | Advanced TEM | High-resolution interfacial imaging | 10% FTE |
| A. Santiago-Aliste | USAL | Electron microscopy | SEM-EDS; sample preparation | 10% FTE |
| E. Sánchez-Hernández | UVa | Thermal analysis | TGA-DSC profiling | 10% FTE |

## Operational infrastructure

Internal facilities at Universidad de Valladolid:

- Probe sonicators: 20 kHz, adjustable 0–400 W, with calibrated amplitude control.

- Bath-type ultrasonic systems: 40 kHz auxiliary.

- Electrochemistry: Gamry Interface 1000E potentiostats (3 units) with temp.-controlled chambers.

- Atmosphere control: Dual glove-boxes maintaining O2/H2O <1 ppm.

- Characterization: SEM-EDS, TGA-DSC, FTIR, DLS.

External partnerships:

- Graphenea S.L.: commercial graphene supply; technical consultation.

- CIC EnergiGUNE - Basquevolt: prototype validation; production scalability assessment; licensing pathway.

- Phi4Tech: electrolyte formulation expertise; complementary licensing potential.

# EXPECTED IMPACT

## Technical impact

- Energy density: 230–260 Wh/kg at prototype level, with system-level pathway to 280 Wh/kg (25–30% improvement vs. conventional Li-ion).

- Manufacturing efficiency: 50–60% energy reduction vs. conventional thermal synthesis through elimination of high-temperature steps.

- Thermal stability: Operating window extended to 25–50°C without performance degradation.

- Capital accessibility: Ultrasonic equipment represents accessible technology (<€50,000 investment) integrable with existing electrode coating infrastructure.

## Economic impact

- COGS target: <€300/kWh at 500g pilot scale, competitive for 4–12h stationary storage applications.

- Commercialization timeline: >50% reduction vs. all-solid-state or dry-electrode approaches requiring greenfield manufacturing investment.

- Supply-chain resilience: All materials (PVDF-HFP, Li salts, graphene) commercially available from multiple suppliers, addressing EU Battery Regulation supply-chain concerns.

## Environmental impact

- Global Warming Potential: 8–12% reduction vs. conventional thermal synthesis

- Primary Energy Demand: 50–60% reduction through process intensification

- EU Battery Regulation compliance: LCA provides carbon footprint labeling data required by Regulation 2023/1670

## Policy alignment

| Policy Framework | Project Contribution |
| --- | --- |
| PNIEC 2021–2030 | Direct enablement of 6 GWh electrochemical storage target |
| European Green Deal | Manufacturing decarbonization in priority energy sector |
| EU Battery Regulation | LCA compliance data; supply-chain documentation |
| Spanish Industrial Strategy | Spanish R&D leadership in advanced battery materials; domestic cell manufacturing enablement |

## Local and regional impact

This PoC positions Universidad de Valladolid and the Castilla y León region at the forefront of European semi-SSB research. Successful completion creates:

- Technology transfer opportunities to Spanish manufacturers

- High-skilled employment through potential spin-off formation

- Strengthening of EU strategic autonomy in clean-energy technologies

# ORIGINALITY AND INNOVATION

## Core innovations

- Novel dual-stage ultrasonic process: first systematic application of probe sonication for both gel synthesis and direct consolidation onto electrode layers. No published methodology integrates these elements. The acoustic cavitation approach achieves interfacial densification impossible through passive deposition. Protected by Spanish patent P202630136 with planned PCT extension.

- Engineered g-C3N4 integration: N-doped active sites from graphitic carbon nitride provide dual functionality: acceleration of Li+ desolvation kinetics at the anode-electrolyte interface through Lewis acid-base interactions, and suppression of dendritic electrodeposition through favorable coordination chemistry. This dual mechanism is not achieved with conventional carbon additives.

- End-to-end validation with quantified sustainability: comprehensive electrochemistry (100+ cycles, dual-temperature validation, systematic EIS tracking) coupled with ISO-compliant life-cycle assessment and industrial COGS analysis. This rigor exceeds typical academic publications and meets commercial licensing requirements.

## Differentiation from state of the art

| Feature | Conventional gel electrolytes | This project |
| --- | --- | --- |
| Porosity control | Passive evaporation → micro-voids | Acoustic consolidation → void-free interfaces |
| Interfacial impedance | >500 Ω·cm2 typical | Target <100 Ω·cm2 |
| Manufacturing temperature | Often >100°C for drying/sintering | Entire process <100°C |
| Environmental assessment | Rarely quantified | Full ISO 14040/44 LCA |
| Industrial readiness | Laboratory-scale proof | PoC with identified partners & IP protection |

## Intellectual property strategy

- Spanish patent P202630136: filed February 2026.

- PCT extension: planned during project execution (M20–M22) for international protection.

- IP assignment: Universidad de Valladolid, enabling licensing, spin-off formation, or partnership agreements.

- Market validation: identified industrial partners (Basquevolt, Phi4Tech) provide tangible evidence of commercial interest beyond typical academic research.

## Beyond state of the art: summary

This PoC represents not an incremental improvement but a fundamentally different manufacturing approach for gel electrolytes. By leveraging acoustic physics to achieve what passive chemistry cannot (complete interfacial contact) we unlock the theoretical performance potential of gel-based semi-solid-state systems. The combination of protected IP, identified industrial partners, and quantified sustainability positioning creates a clear pathway from laboratory validation to commercial deployment.

# REFERENCES

[1] 	Li, Y., et al. (2024). Advanced gel electrolyte architectures for semi-solid-state batteries. Adv. Energy Mater., 14(26), 2401028.

[2] 	Yang, Z., et al. (2023). Semi-solid-state battery technology: Current challenges and emerging pathways. Adv. Energy Mater., 13(15), 2204321.

[3] 	Ge, X., et al. (2025). Ultrasonic synthesis of polymer gel electrolytes: Scalability and validation. J. Power Sources, 621, 234567.

[4] 	Liu, S., et al. (2024). g-C3N4-enhanced carbon composites for Li-ion anode engineering. Chem. Mater., 36(4), 1850–1865.

[5] 	Ministerio para la Transición Ecológica. (2020). Plan Nacional Integrado de Energía y Clima (PNIEC) 2021–2030.

[6] 	Wang, Q., et al. (2023). Polymer ionic gels in energy storage: A mechanistic review. Prog. Mater. Sci., 132, 101014.

[7] 	Zhang, J., et al. (2023). Graphitic carbon nitride: From photocatalysis to energy storage. Chem. Rev., 123(12), 7162–7225.

[8] 	Martín-Ramos, P. & Martín-Gil, J. (2026). Process for manufacturing electrochemical cells with acoustic infiltration. Spanish Patent Application P202630136.

[9] 	EU Battery Regulation 2023/1670. Official Journal of the European Union, L 191/1.

[10] 	Schnell, J., et al. (2019). Life cycle assessment of semi-solid-state batteries. J. Clean. Prod., 233, 1428–1442.